## Slide 1: Flow chemistry for supramolecular processes
Dr Anna Slater (she/her)
University of Liverpool
ETOC
24th Feb 2022

## Slide 2
Email: anna.slater@liverpool.ac.uk Website: agslatergroup.com Twitter: @annagslater
Supra- molecular chemistry
Macrocycles
Self-assembly
Flow Chemistry@Liverpool
Organic materials & precursors
Cages
Polymerisation
How you make something matters as much as the ingredients

## Slide 3
Supramolecular chemistry
…these process can all be profoundly changed by the reaction environment.
Whether making a host,
assembling a host-guest complex,
or forming a supramolecular assembly…
Concentration, mixing, temperature, rate of addition, etc changes yield, selectivity, assembly pathway, kinetic/thermodynamic product selection, thus structure, thus function.
Images: https://en.wikipedia.org/wiki/Supramolecular_chemistry and https://en.wikipedia.org/wiki/Macrocycle

## Slide 4
Tozawa et. al, Nat. Mater., 2009, 8, 973
Change structure, change function
soluble
functionalizable
stable
easy to make
functional

## Slide 5
New pore geometries from self-sorting
ACIE, 2020, 10.1002/anie.202007571
Reticular synthesis via chiral recognition Nat. Chem., 2017, 9, 17-25
Chiral social self-sorting
MSDE, 2018, 3, 223
Flow chemistry
Chem. Comm., 2015, 51, 17390
Change structure, change function

## Slide 6
Scale is tricky due to the use of large amounts of DCM/chloroform
Long reaction times
Complex or unwanted products possible in less well-defined systems
Why does process matter?

## Slide 7
Reduced the reaction time from 5 days to 10 minutes
Same purity, same yield; scalable synthesis
Can telescope with precipitation/crystallisation
Briggs, M. E.;† Slater, A. G.;† Lunt, N.; Jiang, S.; Little, M. A.; Greenaway, R. L.; Hasell, T.; Battilocchio, C.; Ley, S. V. and Cooper, A. I.; Chem. Commun., 2015, 51, 17390-17393
How can flow help?
95 %

## Slide 8
Briggs, M. E.;† Slater, A. G.;† Lunt, N.; Jiang, S.; Little, M. A.; Greenaway, R. L.; Hasell, T.; Battilocchio, C.; Ley, S. V. and Cooper, A. I.; Chem. Commun., 2015, 51, 17390-17393
93 %
What about cages that are harder to access?

## Slide 9
93 %
What about cages that are harder to access?
21 % after prep LC
95 %
Henry Morris (PhD)
Matthew Oakes (MChem)
Caitlin Shields (MChem)
High dilution not required?
Process intensification
Can add TFA catalyst
Product selection
Reaction investigation
Alternative pathways?
Continuous water removal?
Autosamplers and inline detection for cage discovery
Cages can be tricky! Poor solubility of precursors, multiple possible products…but a LOT of fun things to explore looking at reversible chemistry in flow.

## Slide 10
Understanding and optimising selectivity and yield in flow: a macrocyclic molecular hinge
C. D. Jones, L J. K. Cook, D. Marquez-Gamez, K. V. Luzyanin, J. Steed, A. G. Slater, JACS, 2021, 143, 19, 7553-7565
Both isomers formed by an addition cyclisation reaction of 2-bromo- or 2-chloroethylamine with an isocyanate to form oxazolidine rings.
In batch, both isomers formed.
Dr Chris Jones
syn-1
anti-1
syn-2
anti-2

## Slide 11
Batch synthesis
Et3N, CHCl3
Higher T increases yield (76 % at 60 °C) but compromises selectivity – and T limited by solvent.
Can we optimise this synthesis?
C. D. Jones, L J. K. Cook, D. Marquez-Gamez, K. V. Luzyanin, J. Steed, A. G. Slater, JACS, 2021, 143, 19, 7553-7565

## Slide 12
T1 70 °C, T2 90 °C
50 °C
70 °C
100 °C
T1
How can flow help?
C. D. Jones, L J. K. Cook, D. Marquez-Gamez, K. V. Luzyanin, J. Steed, A. G. Slater, JACS, 2021, 143, 19, 7553-7565
Yield tripled, selectivity > 80 %
Platform for diversification
When T1 or T2 are varied, other T is kept constant

## Slide 13
Conclusions
Efficiency
Flow can help with:
Yield
Scalability
Selectivity
Mechanistic understanding
of processes relevant to supramolecular chemistry…
…and there’s lots of space to explore!
Templating
Photoswitching
Droplet synthesis
Rapid ΔT
…
“Enabling technology for supramolecular chemistry”, Katie Ollerton, Rebecca Greenaway & Anna Slater, submitted for International Women in Supramolecular Chemistry special issue, Frontiers in Science, 2021

## Slide 14
Acknowledgements
Slater Group
Dr Firdaus Parveen, Henry Morris, Abbie Scholes, Megan Carr, Patrycja Roszkowska, Nick Watson, Caitlin Shields, Matthew Munro, Charlotte Hutchison
Dr Chris Jones, Dr Valentina Abet, Matthew Oakes
Collaborators
Prof Andy Cooper, Dr Kim Jelfs, Prof Jon Steed, Prof Rich Bourne, Dr Michael Briggs, Dr Marc Little, Dr Konstantin Luzyanin, Dr Laurence Kershaw-Cook, Dr David Marquez-Gamez, Dr Becky Greenaway, Dr Claudio Battilocchio, Prof Steven Ley
Thank you for your attention!
Email: anna.slater@liverpool.ac.uk Website: agslatergroup.com Twitter: @annagslater